| ### Item | ### Description |
| --- | --- |
| ###### H01 a. ###### H02 a. b. c. d. e. f. g. h. i. j. ###### H03 a. | ## GENERAL REQUIREMENTS Definitions Similar Approved:; Specification requirements of products should be met at all times. Other manufacturers may be considered on producing the same specification requirements as laid out in the schedule of works, subject to approval from the Contract Administrator.. ## Code of Practice Comply with all relevant Codes of Practice, subject to any qualifications given below. ## MATERIALS Insitu-Finishes Ordinary or rapid hardening Portland Cement shall be to BS 12: Part 2. Portland blast furnace cement shall be to BS 146: Part 2. Sand for cement rendering shall be to BS 1199, Table 1. Fine aggregate shall be to BS 882: Part 2, Table 2, graded to zones 1, 2 or 3. Coarse aggregate shall be to BS 882: Part 2, Table 1 Bonding agent shall be a type recommended by manufacturer of plaster, or approved. Water shall be clean and fresh. Steel lathing shall be to BS 1369: - Plain expanded type. - Minimum weight 1.6 kg/m unless otherwise specified. - Painted with black bitumen solution Gypsum lath shall be to BS 1230. Steel clout nails shall be to BS 1202: Part 1, Table 3, galvanised to BS 729. ## WORKMANSHIP Insitu-Finishes Code of Practice for plastering/rendering shall unless otherwise specified comply with the following sections of BS 5492: |

| ### Item | ### Description |
| --- | --- |
| b. c. d. e. f. g. | - Section 1: General - Section 3: Backgrounds - Section 5: Application - Section 6: Maintenance Code of Practice for concrete floor finishes shall unless otherwise specified comply with CP 204. Mixes: Cement Aggregate; 1:3. Fine Concrete; 1:1:5 Cement: Fine Aggregate: Coarse Aggregate 10mm maximum. Rendering Externally; 1:1:5 Cement: Lime: Sand. Preparation of Concrete and Brickwork to be as follows: - - Hack off projections and fins. - Clean the surfaces of all dust, loose particles and other matter. - Remove laitance or efflorescence (by dry methods) and remove any grease or oil completely. - Provide an adequate key to receive the render specified. Steel lathing to be fixed as follows: - Lap joints 75mm and wire at intervals not exceeding 75mm. - Fix to timber with 32mm galvanised cut staples. - Fix to steelwork with 1.2mm galvanised wire. Plain finish render to be applied as follows: - - To a uniform thickness with laying trowel. - Finish with a wood or other suitably faced float to give an even texture. Scrapped Finish Render to be applied as follows: - - To a uniform thickness with a laying trowel. - After coat has set but before too hard, expose aggregate by scraping surface skin to approved texture. |

| ### Item | ### Description |
| --- | --- |
| ###### H04 a. b. c. d. e. f. g. h. ###### H05 a. ###### H06 a. | ## Wall Tiling Ensure that plaster is dry, solidly bedded and free from dust and friable matter. Remove soft or flaking paint by mechanical / manual means. Do not use chemical paint strippers. Wall tiling shall be carried out in accordance with BS 5385 and Fix with approved waterproof adhesive in accordance with recommendations of adhesive manufacturers, joints to line up horizontally and vertically. Tiles around sockets and reveals shall be cut neatly using the appropriate tile saw. Apply adhesive as a continuous screed to a thickness of approximately 3mm on the surface to be tiled but not more than 1m2 at a time to prevent premature drying out. Press tiles onto the adhesive and tap firmly into position to ensure solid bedding without voids. Make any necessary adjustment to tiles immediately after bedding. Clean off tiles as soon as bedding is complete. Joints between tiles shall be filled solid with an approved waterproof grout. The joints shall be tooled off and on completion all residual adhesive and grout shall be cleaned off the tiles and surrounding surface. Vinyl and Thermoplastic Tiles Workmanship shall comply with the recommendations of BS 8203. Tiles shall unless otherwise directed be laid with straight joints on a combed bed of appropriate approved adhesive strictly in accordance with the recommendations of the manufacturers of the tiles and adhesive respectively. The size, colour and pattern of the tiles shall match as near as possible any existing surrounding tiles and in any case must be to the entire satisfaction of the Contract Administrator. The rates for laying tiles include the making good of damaged sub-floors with an approved proprietary self-levelling latex cement compound. Quarry Tiles Workmanship shall be in accordance with BS 5385 part 3. The tiles shall be laid on bed of cement and sand (1:3), or on approved cementitious adhesive bed 3-6mm thick, which must make full contact with the tile and background and be in accordance with the recommendations of the adhesive manufacturer. |